CERTIFICATE OF ANALYSIS

| Product： | Gelatin | Bath NO.： | AQ20200717 |
| --- | --- | --- | --- |
| Manufacture Date: | 2020.07.17 | Valid Date: | 2022.07.16 |
| Pack: | 25KG/BAG | Quantity : | 1000KG |
| Sample date： | 2020.07.17 | Analysis date： | 2020.07.26 |
| Technical specification： | CP 2015 |  |  |

| Test items | Analytical methods | Standard | Result | Result found |
| --- | --- | --- | --- | --- |
| Appearance (25℃) | CP 2015 | This product is yellowish to yellow, transparent or translucent microstrip glossy thin flakes or powder; Odorless, tasteless; When immersed in water, it expands and becomes soft, absorbing 5 to 10 times its own mass of water, This product is soluble in hot water, soluble in acetic acid or glycerin and water in the hot mixture, insoluble in ethanol | Conforms | Qualified |
| Identification | CP 2015 | (1)Take 0.5g of this product, add 50ml water, heat to dissolve, take 5ml solution, add potassium chromate test solution- Dilute hydrochloric acid (4:1) a few drops, namely the formation of orange flocculent precipitation | Conforms | Qualified |
|  |  | (2)Take 1ml of the remaining solution under item (1), add 100ml water, shake well, add several drops of tannic acid test solution, then turbidity will occur | Conforms | Qualified |
|  |  | - (3)Add sodium lime and heat it to produce ammonia odour | Conforms | Qualified |
| Intensity of frozen force(6.67%) | CP 2015 | ≥180 | 194 | Qualified |
| PH | CP 2015 | 4.0-7.2 | 5.4 | Qualified |
| Light transmittance%,620nm | CP 2015 | ≥70 | 90 | Qualified |
| Electrical conductivity,ms/cm | CP 2015 | ≤0.5 | 0.1 | Qualified |
| Sulfites(SO2),% | CP 2015 | ≤0.01 | <0.01 | Qualified |
| Peroxide,in 10g | CP 2015 | Not blue | Conforms | Qualified |
| Loss on drying,% | CP 2015 | ≤15.0 | 11.2 | Qualified |
| Residue on ignition,% | CP 2015 | ≤2.0 | 0.5 | Qualified |
| Chromium,mg/kg | CP 2015 | ≤2.0 | 0.3 | Qualified |
| Heavy metal,% | CP 2015 | ≤0.003 | <0.003 | Qualified |
| Arsenic salt,% | CP 2015 | ≤0.0001 | <0.0001 | Qualified |
| Viscosity(6.67%,60℃),mPa·S | CP 2015 |  | 3.85 | Qualified |
| Viscosity(6.67%,37℃),% | CP 2015 |  | 2.7 | Qualified |
| Total aerobic bacteria,cfu/g | CP 2015 | ≤1000 | 57.3% | Qualified |
| Total Mold and yeast,cfu,g | CP 2015 | ≤100 | 36.7% | Qualified |
| Escherichia coli,in 1g | CP 2015 | ND | Conforms | Qualified |
| Salmonella,in 10g | CP 2015 | ND | Conforms | Qualified |
| Conclusion | In accordance with CP 2015 |  |  |  |

QC Supervisor: Liuxixia       Recheck:   Jinchangyun       Analyst:  Li Hong