检验报告单

Certificate Of Analysis

执行标准(Criterion):Q/B

| 检品名称 Commodity Name | 甲基丙烯酸-9-蒽甲酯 9-Anthracenylmethylmethacrylate | CAS No. |  | 31645-35-9 |
| --- | --- | --- | --- | --- |
| 复检日期 Retest Date | 2024年07月30日 | 批号 Batch NO. |  | RJ276-TM-202307 |
| 生产日期 Manufacturer Date | 2023年07月31日 | 失效日期 Expiry Date |  | 2025年07月30日 |
| 包装规格 Packegingspecifications | 11kg/桶 | 数量 Batch Size |  | 11kg |
| 检验依据 Test based | 本品依据“企业标准”标准检验 The results of product testing standards in line with “company standard”. |  |  |  |
| 检验项目 Testing Item | 标准规定 Standard requirments |  | 检验结果 Test results |  |
| 【外观】 Appearance 【纯度】 Purity | 淡黄色粉末 Light Yellow Powder 99.5% min |  | 符合 Complies 符合 Complies |  |
| 【单杂】 Single impurity | HPLC图谱中10.748min杂质（产品8.133min ）小于0.05% Impurities (product peak 8.133min) less than 0.05% in HPLC spectrum at 10.748min |  |  |  |
| 【溶解性】 Solubility | 溶解于1%丙二醇甲醚溶液，为无色澄清溶液 Dissolved in 1% propylene glycol methyl ether solution, it is a colorless and clear solution |  |  |  |
| 【储存条件】 Storage conditions | 避光、低温保存 Protected from light and stored at low temperature |  |  |  |
| 结 论 Determination | 标准检验符合规定。 The results of product testing standards in line |  |  |  |
| 判 定 Result |  |  | 合 格 Complies |  |

报告人：                   复核人：                  审核人：

Reported  by：                 Reviewed by：                 Approved by：